# GUIDE SPECIFICATION

# PAC-Shield Nail Base

August 2024

## SECTION 07 21 13 - NAIL BASE INSULATION PANELS

** NOTE TO SPECIFIER **

Display hidden notes to specifier by using “Tools”/”Options”/“View”/”Hidden Text”.

Follow the instructions listed in the ** NOTE TO SPECIFIER ** sections included throughout the specification. Edit carefully to suit project requirements. Modify as necessary and delete paragraphs that are not applicable.

This section is based on the products of Petersen Aluminum Corporation, which is located at:

1005 Tonne Road

Elk Grove Village, IL 60007 Phone: (800) PAC-CLAD

Fax: (800) 722-7150

E-mail: info@pac-clad.com Internet: www.pac-clad.com

Petersen Aluminum Corporation is the developer and producer of high performance ventilated nailbase insulation panels for steep slope roofing applications greater than 3 inches in 12 inches. A universally accepted substrate for all major types of roof coverings, PAC-Shield Nail Base offers superior compressive strength, competitive pricing and the highest R-value per inch of any insulating material on the planet.

Our products complement the development of sustainable design practices and fundamentally enhance the building's effectiveness in the environment by reducing energy consumption. Our products components include OSB and plywood that are USGBC certified and our insulating foam contains a recycled content to promote sustainable design practices and significantly reduce energy consumption. It's our way of helping keep the world green.

GENERAL

SECTION INCLUDES

Section includes nailbase insulation panel system.

RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete sections below not relevant to this project; add others as required.

Section 05300 – Steel Deck.

Section 06110 - Wood Framing: Structural deck sheathing.

Section 06114 - Wood Blocking.

Section 06150 - Plywood Decking.

Section 07260 - Vapor Retarders.

Section 07310 - Roof Shingles.

Section 07320 - Roof Tiles.

REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

ASTM C 209 – Methods of Testing Insulating Board, Structural and Decorative.

ASTM C 1289 – Specifications for Faced Rigid Cellular Polyisocyanurate Thermal Insulating Board.

ASTM D 1621 – Test Methods for Compressive Properties of Rigid Cellular Plastics.

ASTM D 2126 - Test Method for Response of Rigid Cellular Plastics to Thermal and Humid Aging.

ASTM E 84 – Surface Burning Characteristics of Building Materials.

ASTM E 96 - Test Method for Water Vapor Transmission of Materials.

CAN/ULC S770 - Standard Test Method for Determination of Long Term Thermal Resistance of Closed Cell Plastic Thermal Insulating.

UL 1256 - Fire Test of Roof Deck Constructions.

PS2-92 - Performance Standard for Wood-based Structural-use Panels.

FM 4450 - Class I Insulated Steel Deck Roofs.

FM 4470 - Class I Roof Covers (Foam Core Only).

FM Class 1 approval for steel roof deck constructions, Class 1 Fire and I-60 and I-90 wind storm classifications

Florida Building Code Approval FL# 46425

Miami Dade Product Control – Notice of Acceptance NOA No. 23-1208.14

SYSTEM DESCRIPTION

Physical properties (Foam Core):

Manufactured using 3rd Generation Zero ODP, EPA Compliant Blowing Agent; Contains zero CFCs, HCFCs, or HFCs; Virtually no Global Warming Potential (GWP)

Compressive Strength: ASTM D 1621 and ASTM C 1289, Type V, Class 1, 20 psi

(138 kPa) minimum for Grade 2

Dimensional Stability: ASTM D 2126, 2 percent linear change (7 days).

Moisture Vapor Transmission: ASTM E 96, < 1 perm ((57.5ng/(Pasm2)).

Water Absorption: ASTM C 209, < 1 percent by volume.

Service Temperature: Minus 100 degrees to 250 degrees F (Minus 73 degrees C to 122 degrees C).

Foam core flame spread index of 75 or less and smoke developed of 450 or less when tested in accordance with ASTM E 84.

Foam Core R Values: Based on LTTR (Long Term Thermal Resistance) in accordance with ASTM C 1289.

UL Assemblies: Insulated steel deck assemblies - UL 1256 (nos. 120, 123).

UL Assemblies: Insulated steel deck assemblies - UL 1256 (nos. 120, 123) TGDY. R20624 Shingle Deck Accessory; PAC-Shield Nail Base roof insulation is classified for use with any Class A, B, or C asphalt glass mat or asphalt organic shingles, standing seam metal or tile roof coverings.

** NOTE TO SPECIFIER ** Use the following three paragraphs to identify system performance requirements or functional criteria. Delete references that are not actually required.

FM Class 1 (Low Slope) approval for steel roof deck constructions, Class 1 Fire and I-60 and I-90 wind storm classifications.

Hail Rating: SH-1 and VSH

SUBMITTALS

Submit under provisions of Section 01300.

Product Data: Manufacturer's data sheets on nailbase insulation panels and fasteners to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

** NOTE TO SPECIFIER ** Delete the following paragraphs if LEED is not applicable.

LEED Submittals: Provide documentation of how the requirements of Credit will be met:

List of proposed materials with recycled content. Indicate post-consumer recycled content and pre-consumer recycled content for each product having recycled content.

Manufacturer-Specific Environmental Product Declaration which conforms to ISO 14025

Verification Samples: For each finish product specified, two samples, representing actual product.

Submit 6 by 6 inch (152 mm by 152 mm) samples of each board type required.

Submit samples of each fastener type required.

Manufacturer's Certificate: Certify nailbase insulation panels will conform to specified performance requirements.

QUALITY ASSURANCE

Manufacturer Qualifications: Manufacturer shall be a company that regularly manufactures polyisocyanurate and fully assembles nailbase insulation panels in-house with no outside fabrication operations.

Manufacturer shall have multiple manufacturing facilities to ensure consistency of product supply.

DELIVERY, STORAGE, AND HANDLING

Good construction practice dictates that all insulations should be protected from moisture and direct sunlight during job-site storage. Pallets of PAC-Shield Nail Base are protected by a 2-step packaging process using shrink wrap and a UV resistant polyethylene bag. This moisture resistant package is designed for protection from the elements during flatbed shipment from our facilities to the job-site.

Store products in accordance with the manufacturer recommendations.

Store product on a solid flat foundation and elevate a minimum of 2 inches above the finished surface.

Slit the bundle packaging vertically down the center of the two short sides and cover with a waterproof tarpaulin

Protect insulation from open flame and keep dry at all times.

PROJECT CONDITIONS

Install only as much insulation as can be covered the same day by a completed roof covering material.

PRODUCTS

MANUFACTURERS

Basis of Design: PAC-Shield Nail Base produced by Petersen Aluminum Corporation, 1005 Tonne Road, Elk Grove Village, IL 60007. Phone: (800) PAC-CLAD. Fax: (800) 722-7150. E-mail: info@PAC-CLAD.com. Web: www.PAC-CLAD.com.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

Substitutions: Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600.

** NOTE TO SPECIFIER ** Select the required panel paragraphs from the following list. Delete the paragraphs not required. If more than one product is required identify the location of the materials required on the Drawings. For slate and tile roofs, PAC-Shield Nail Base with plywood is recommended. PAC-Shield Nail Base may be used on non-mechanically attached low slope assemblies but must be manufactured online without the use of glue and have an OSB top layer.

PANEL CONSTRUCTION

Board Insulation: Provide products that comply with the following:

** NOTE TO SPECIFIER ** Delete all of the following standards that are not required; coordinate with product specifications.

ASTM standards specified.

Factory Mutual (FM) approvals specified.

Underwriters Laboratories Inc. (UL) classifications specified.

Florida Building Code Approval FL# 46425.

Miami Dade County, Florida Product Control No. 23-1208.14.

ICC – ESR-1455

Panels shall consist of a top layer of APA/TECO rated Oriented Strand Board (OSB) core that is laminated, on-line, to a bottom layer of fiber-reinforced facers (GRF) polyisocyanurate foam insulation.

Polyisocyanurate foam insulation shall conform to ASTM C 1289, Type V.

** NOTE TO SPECIFIER ** Select one of the following two paragraphs and delete the one not required.

Compressive Strength: 20 pounds per square inch (138 kPa) Grade 2.

OSB Top layer substrate shall conform to PS2 and shall be as follows:

OSB:

** NOTE TO SPECIFIER ** Select one of the two following OSB types and delete the paragraph that is not required. Include FSC type if LEED certification is required.

Type:

Standard sheathing grade.

** NOTE TO SPECIFIER ** Select one of the following OSB thicknesses and delete the paragraphs that are not required.

Thickness:

7/16 inch (11.1 mm).

5/8 inch (15.9 mm).

** NOTE TO SPECIFIER ** Select one of the following edge detail paragraphs and delete the one not required.

Edge detail (provide description)

Rabbeted.

Non-rabbeted.

Panels shall consist of a top layer of APA exterior grade 5-ply CDX plywood laminated off-line to fiber-reinforced facers (GRF) polyisocyanurate foam insulation.

Polyisocyanurate foam insulation shall conform to ASTM C 1289, Type V with a compressive strength of:

Grade 2: 20 psi (138 kPa) minimum).

5-ply CDX Plywood Top layer substrate shall conform to PS2 and shall be as follows:

** NOTE TO SPECIFIER ** Select one of the two following plywood types and delete the paragraph that is not required. Include the third paragraph FSD LEED certification if required.

Type:

Standard sheathing grade.

5-ply Fire-treated sheathing grade.

** NOTE TO SPECIFIER ** Select one of the following plywood thicknesses and delete the paragraphs that are not required.

Thickness:

5/8 inch (15.9 mm).

3/4 inch (19.0 mm).

** NOTE TO SPECIFIER ** Select one of the following edge detail paragraphs and delete the one not required.

Edge detail:

Rabbeted.

Non-rabbeted.

** NOTE TO SPECIFIER ** Select one of the following panel types and delete the paragraphs that are not required. The first paragraph refers to panels with a top layer substrate thickness of 7/16 inch (11.1 mm) or /8 inch (15.9 mm). The second paragraph refers to panels with a top layer thickness of 3/4 inch (19 mm).

PANEL TYPES

PAC-Shield-Nail Base panels 7/16 inch (11 mm) OSB shall be 47-1/2 inches by 95-1/2 inches (1207 mm by 2426 mm) with an overall thickness, R-value, and flute spanability as follows:

** NOTE TO SPECIFIER ** Select the required panel thickness paragraph from the following list. Delete the paragraphs not required. When a foam thickness of 3.5 inch or greater is required, a two layer system with staggered joints is recommended. Also, If more than one thickness is required identify the location of the materials required on the Drawings.

Thickness 1.5 inches (38 mm), R Value 6.3, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.0 inches (51 mm), R Value 9.2, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.5 inches (64 mm), R Value 12. 0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.0 inches (76 mm), R Value 15. 0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.5 inches (89 mm), R Value 18.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 4.0 inches (102 mm), R Value 21.1, flute spanability 4-3/8 inches

(111.13 mm).

PAC-Shield-Nail Base panels 5/8 inch (16 mm) OSB foam size shall be 47-1/2 inches by 95-1/2 inches (1207 mm by 2426 mm) with an overall thickness, R-value, and flute spanability as follows:

** NOTE TO SPECIFIER ** Select the required panel thickness paragraph from the following list. Delete the paragraphs not required. When a foam thickness of 3.5 inch or greater is required, a two layer system with staggered joints is recommended. Also, If more than one thickness is required identify the location of the materials required on the Drawings.

Thickness 1.6 inches (41 mm), R Value 6.3, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.1 inches (53 mm), R Value 9.2, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.6 inches (66 mm), R Value 12.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.1 inches (79 mm), R Value 15.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.6 inches (91 mm), R Value 18.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 4.1 inches (104 mm), R Value 21.1, flute spanability 4-3/8 inches

(111.13 mm).

PAC-Shield-Nail Base panels 5/8 inch (16 mm) 5-ply CDX plywood foam size shall be 48 inches by 96 inches (1220 mm by 2438 mm) with an overall thickness, R-value, and flute spanability as follows:

** NOTE TO SPECIFIER ** Select the required panel thickness paragraph from the following list. Delete the paragraphs not required. When a foam thickness of 3.5 inch or greater is required, a two layer system with staggered joints is recommended. Also, If more than one thickness is required identify the location of the materials required on the Drawings.

Thickness 1.6 inches (41 mm), R Value 6.3, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.1 inches (53 mm), R Value 9.2, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.6 inches (66 mm), R Value 12.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.1 inches (79 mm), R Value 15.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.6 inches (91 mm), R Value 18.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 4.1 inches (104 mm), R Value 21.1, flute spanability 4-3/8 inches

(111.13 mm).

PAC-Shield-Nail Base panels 3/4 inch (19 mm) 5-ply CDX plywood foam size shall be 48 inches by 96 inches (1220 mm by 2438 mm) with an overall thickness, R-value, and flute spanability as follows:

** NOTE TO SPECIFIER ** Select the required panel thickness paragraph from the following list. Delete the paragraphs not required. When a foam thickness of 3.5 inch or greater is required, a two layer system with staggered joints is recommended. Also, If more than one thickness is required identify the location of the materials required on the Drawings.

Thickness 1.7 inches (43 mm), R Value 6.3, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.2 inches (56 mm), R Value 9.2, flute spanability 4-3/8 inches 
(111.13 mm).

Thickness 2.7 inches (69 mm), R Value 12.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.2 inches (81 mm), R Value 15.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 3.7 inches (94 mm), R Value 18.0, flute spanability 4-3/8 inches

(111.13 mm).

Thickness 4.2 inches (107 mm), R Value 21.1, flute spanability 4-3/8 inches

(111.13 mm).

PANEL FASTENERS

** NOTE TO SPECIFIER ** Select one of the two following fastener substrate paragraphs and delete the paragraph that is not required. Include both if more than one substrate is required.

Fasteners shall be FM Approved Petersen Aluminum Corporation SIP/SD Panel Fasteners for steel deck application. Fasteners have a 3/16 inch (5 mm) shank, and are corrosion resistant with oversized heads. Length of fasteners shall be as recommended by Petersen Aluminum Corporation. Use of 2 inch (51 mm) round plates are not required. See the Petersen Aluminum Corporation application guide for instructions.

Penetration of fastener into bottom flute is not acceptable.

Fasteners shall be FM Approved Petersen Aluminum Corporation SIP/WD Panel fasteners for wood deck application. Fasteners have a 3/16 inch (5 mm) shank, and are corrosion resistant with oversized heads. Length of fasteners shall be as recommended by Petersen Aluminum Corporation. Use of 2 inch (51 mm) round plates are not required. See the Petersen Aluminum Corporation application guide for instructions.

EXECUTION

** NOTE TO SPECIFIER ** See Petersen Aluminum Corporation Installation Guide for recommended fastening patterns and installation methods. Coordinate roof covering installation requirements with roof covering manufacturer.

EXAMINATION

Do not begin installation until substrates have been properly prepared.

Verify deck, adjacent materials, and structural backing is dry and ready to receive insulation.

Verify deck surface is flat, free of fins, protrusions and irregularities.

If deck preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

PREPARATION

Clean surfaces thoroughly prior to installation.

** NOTE TO SPECIFIER ** The incorporation of a vapor barrier or retarder within the roofing assembly is highly recommended when the project is located in Zones 1, 2 or 3 of the United States. PAC-Shield is not intended to substitute for a vapor barrier. Vapor barrier or retarder when used shall have a perm rating of 0.5 or less as determined by ASTM E-96.

Apply vapor barrier and or retarder, as specified by the Architect or required by the local building code, to decking prior to the installation.

INSTALLATION

Install in accordance with manufacturer's instructions.

For multiple layered installations, install the base layer of panels loose-laid, and stagger the joints of subsequent layers in accordance with good roofing practice. Fasten panels through the top nailable surface and also through the wood block panel spacers using Petersen Aluminum Corporation approved threaded fasteners.

For adhered low slope installations, apply panels in hot asphalt or cold adhesive using only PAC-Shield Nail Base with OSB. Contact finished roof manufacturer for details.

Only install enough PAC-Shield-Nail Base per day that can be covered the same day by a completed roof covering material.

Use only UL or FM approved synthetic underlayment over nailbase insulation panels. The use of 15 or 30 pound roofing felt is not recommended.

PROTECTION

Protect installed products until completion of project.

Touch-up, repair or replace damaged products before Substantial Completion.

Cover the top and edges of unfinished roof panel work to protect it from the weather and to prevent accumulation of water in the cores of the panels.

END OF SECTION