# GUIDE SPECIFICATION

# PAC-Shield CI Nail Base

August 2024

## SECTION 07 21 13 - CONTINUOUS INSULATION WALL PANELS

** NOTE TO SPECIFIER **

Display hidden notes to specifier by using “Tools”/”Options”/“View”/”Hidden Text”.

Follow the instructions listed in the ** NOTE TO SPECIFIER ** sections included throughout the specification. Edit carefully to suit project requirements. Modify as necessary and delete paragraphs that are not applicable.

This specification is based on the continuous insulation products of Petersen Aluminum Corporation, located at:

1005 Tonne Road

Elk Grove Village, IL 60007 Phone: (800) PAC-CLAD

Fax: (800) 722-7150

E-mail: info@pac-clad.com Internet: www.pac-clad.com

Petersen Aluminum Corporation is the developer and producer of high performance polyisocyanurate insulation panels for the interior or exterior of structural exterior walls of residential and commercial buildings. Pac-Shield CI products are designed for use in commercial and residential wall applications to provide “ci” continuous insulation within the building envelope.

This specification includes PAC-Shield CI Nail Base, an energy efficient rigid insulation panel composed of a closed cell polyisocyanurate foam core bonded to a premium performance coated glass facer on one side and OSB (7/16” or 5/8”) or 5-ply plywood (5/8” or ¾”) on the other. It is designed for use in exterior wall assemblies of Type V buildings to provide both continuous insulation and a cladding attachment substrate. In specific wood stud applications this panel can be used as structural sheathing.

GENERAL

SECTION INCLUDES

PAC-Shield CI Nail Base Continuous Insulation Composite Panels for Exterior Walls.

** NOTE TO SPECIFIER ** - Delete any paragraphs below not applicable to project

RELATED SECTIONS

Section 03300 - Cast in Place Concrete: Concrete base wall.

Section 03400 - Pre-Cast Concrete: Pre-cast concrete base wall.

Section 04210 - Clay Masonry: Brick facing.

Section 04800 - Masonry Assemblies: Masonry base wall.

Section 04850 - Stone Facing.

Section 05400 - Cold Formed Metal Framing.

Section 07260 - Vapor Retarders: Vapor retarder materials over insulation to adjacent insulation.

Section 07270 - Air Barriers: Air seal materials over insulation to adjacent insulation.

Section 09110 - Non-Structural Metal Framing.

Section 09200 - Plaster and Gypsum Board.

Section 09220 - Stucco.

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section; add others as required.

REFERENCES

ASTM C 209 - Methods of Testing Insulating Board, Structural and Decorative.

ASTM C 518 - Steady State Thermal Transmission By Means Of The Heat Flow Meter Apparatus (R Value)

ASTM C 1289 – Specifications for Faced Rigid Cellular Polyisocyanurate Thermal Insulating Board.

ASTM D 1621 – Test Methods for Compressive Properties of Rigid Cellular Plastics.

ASTM D 2126 - Test Method for Response of Rigid Cellular Plastics to Thermal and Humid Aging.

ASTM D 3273 - Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E 96 - Test Method for Water Vapor Transmission of Materials.

ASHRAE 90.1- Energy Standard for Buildings Except Low-Rise Residential Buidlings

IBC Chapter 26- Foam Plastic

UL 263- Standard for Fire Tests of Building Construction and Materials

** NOTE TO SPECIFIER ** - Delete sections below not relevant to this project; add others as required.

DESIGN REQUIREMENTS

Perform work in accordance with all federal, state and local codes.

Physical properties (Foam Core):

Flame Spread Index: ASTM E 84; less than 75

Smoke Developed: ASTM E 84; less than 450.

Compressive Strength: ASTM D 1621; Grade 2 (20psi / 138 kPa) or Grade 3 (25psi / 172 kPa).

Dimensional Stability: ASTM D 2126, 2 percent linear change (7 days).

Moisture Vapor Permeance: ASTM E 96, less than 1 perm (57.5ng/(Pa•s•m2)).

Water Absorption: ASTM C 209, less than 0.1 percent by volume.

Service Temperature: Minus 100 degrees to 250 degrees F (Minus 73 degrees C to 122 degrees C).

Resistance to Mold: ASTM D 3273 Passed (10).

3rd Generation Zero ODP Blowing Agent; Contains zero CFCs, HCFCs, or HFC; Virtually no Global Warming Potential (GWP)

OSB or Plywood substrate:

Flame Spread Index: ASTM E84; less than 75

Smoke Developed: ASTM E84; less than 450

Plywood is 5-ply CDX

ASTM C1289 Type V panel (foam core is Type 2, Class 2)

PAC-Shield CI Nail Base is evaluated and listed under DrJ TER 2404-02. Test include:

Structural shearwall attachment of PAC-Shield CI Nail Base to wood studs. Limited panel thicknesses for this application.

PAC-Shield CI Nail Base has passed the following:

Meets the current continuous insulation standards of ASHRAE 90.1, IECC, and IBC Chapter 26

UL 263 Time-Rated Assemblies

SUBMITTALS

Submit under provisions of Section 01300.

Product Data: Manufacturer's data sheets and installation guides on wall panels and fasteners, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Fastening Guidelines: Manufacturer’s 3rd party engineering evaluations for attachment of PAC-Shield CI Nail Base.

** NOTE TO SPECIFIER ** - Delete the following paragraphs if LEED is not applicable.

LEED Submittals: Provide documentation of how the requirements of Credit will be met:

List of proposed materials with recycled content. Indicate post-consumer recycled content and pre-consumer recycled content for each product having recycled content.

Manufacturer Specific Environmental Product Declaration which conforms to ISO 14025 and Polyisocyanurate Insulation Manufacturers Association EPD

Manufacturer's Certificate: Certify panels will conform to specified performance requirements.

QUALITY ASSURANCE

Manufacturer Qualifications: Manufacturer shall be a company that regularly manufactures and assembles specified insulation in house with no outside fabrication operations.

Pre-Installation Meeting: Convene minimum one week prior to commencing Work of this section. Review installation procedures and coordination required with Related Work and include the following:

Participants: Authorized representatives of the Contractor, Architect, Installer, and Manufacturer.

Review wall assemblies for potential interference and conflicts and coordinate layout and support provisions for interfacing work.

Review continuous insulation wall panels installation methods and procedures related to application, including manufacturer’s installation guidelines.

Review firestopping requirements and weather resistive membrane requirements and placement locations.

Review field quality control procedures.

DELIVERY, STORAGE, AND HANDLING

Good construction practice dictates that all insulations should be protected from moisture and direct sunlight during job-site storage. Pallets of PAC-Shield CI Nail Base are protected with a two-step packaging process using stretch wrap and a UV resistant polyethylene bag. This moisture resistant package is designed for protection from the elements during flatbed shipment from our factories to the job-site. Outdoor storage for extended periods of time requires waterproof tarpaulins and elevated storage above ground level a minimum of 2”. Additionally, we recommend slitting the bundle packaging vertically down the center of the two short sides to prevent moisture accumulation within the package.

SEQUENCING

Coordinate with the installation of vapor retarders and air seal materials specified is Section 07260 and Section 07270.

Ensure that products of this section are supplied to affected trades in time to prevent interruption of construction progress.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits.

PRODUCTS

MANUFACTURERS

Basis of Design: PAC-Shield CI Nail Base produced by Petersen Aluminum Corporation, 1005 Tonne Road, Elk Grove Village, IL 60007. Phone: (800) PAC-CLAD. Fax: (800) 722-7150. E-mail: info@pac-clad.com.

** NOTE TO SPECIFIER ** - Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

Substitutions: Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600.

BOARD INSULATION

Roof Board Insulation: Provide products that comply with the following:

** NOTE TO SPECIFIER ** Delete all of the following standards that are not required; coordinate with product specifications.

ASTM standards specified.

Factory Mutual (FM) approvals specified.

Underwriters Laboratories Inc. (UL) classifications specified.

DrJ TER 2404-02

Board Insulation Bonded to OSB or Plywood: PAC-Shield CI Nail Base is an energy efficient rigid insulation panel composed of a closed cell polyisocyanurate foam core bonded to a premium performance coated glass facer on one side and OSB or plywood on the other.

Foam core:

Grade 2 (20 psi).

Grade 3 (25 psi).

Wood Panel Thickness:

7/16 inch Oriented Strand Board (OSB).

5/8 inch Oriented Strand Board (OSB).

5/8 inch Plywood.

3/4 inch Plywood

Panel Size:

4 feet by 8 feet (1220 mm by 2440 mm).

Thickness / R Value: based on ASTM C 518 at 75 degrees F (23.9 degrees C)

1.5 inches (41 mm) / R Value 6.6 with 7/16 inch OSB facing

1.6 inches (42 mm) / R Value 6.6 with 5/8 inch OSB facing

1.6 inches (42 mm) / R Value 6.8 with 5/8 inch plywood facing

1.7 inches (43 mm) / R Value 7.0 with 3/4 inch plywood facing

2.0 inches (53 mm) / R Value 9.6 with 7/16 inch OSB facing

2.1 inches (54 mm) / R Value 9.6 with 5/8 inch OSB facing

2.1 inches (54 mm) / R Value 9.8 with 5/8 inch plywood facing

2.2 inches (56 mm) / R Value 10.0 with 3/4 inch plywood facing

2.5 inches (65 mm) / R Value 12.7 with 7/16 inch OSB facing

2.6 inches (66 mm) / R Value 12.7 with 5/8 inch OSB facing

2.6 inches (66 mm) / R Value 12.9 with 5/8 inch plywood facing

2.7 inches (69 mm) / R Value 13.1 with 3/4 inch plywood facing

3.0 inches (76 mm) / R Value 15.9 with 7/16 inch OSB facing

3.1 inches (79 mm) / R Value 15.9 with 5/8 inch OSB facing

3.1 inches (79 mm) / R Value 16.1 with 5/8 inch plywood facing

3.2 inches (81mm) / R Value 16.3 with 3/4 inch plywood facing

3.5 inches (89 mm) / R Value 19.1 with 7/16 inch OSB facing

3.6 inches (91 mm) / R Value 19.1 with 5/8 inch OSB facing

3.6 inches (91 mm) / R Value 19.3 with 5/8 inch plywood facing

3.7 inches (94 mm) / R Value 19.5 with 3/4 inch plywood facing

4.0 inches (102 mm) / R Value 21.7 with 7/16 inch OSB facing

4.1 inches (104 mm) / R Value 21.7 with 5/8 inch OSB facing

4.1 inches (104 mm) / R Value 22.5 with 5/8 inch plywood facing

4.2 inches (107 mm) / R Value 22.7 with 3/4 inch plywood facing

Provide to the thickness indicated on the Drawings.

PANEL FASTENERS

Fasteners shall be approved Petersen Aluminum Corporation fasteners. Fasteners are a corrosion resistant type with oversized heads. Length of fasteners shall be as recommended by the panel manufacturer.

SIP/HD and SIP/HD-PT (Partial Thread): 12-16 gauge steel studs

SIP/SD and SIP/SD-PT (Partial Thread): 18-22 gauge steel studs

SIP/SD: Concrete and CMU (pre-drilling required)

SIP/WD: Wood studs

SIP/WD: Concrete and CMU (pre-drilling required)

Engineering Evaluations for fastening patterns.

WRB

Vapor permeable barrier recommended for exterior of PAC-Shield CI Nail Base panels (10- 60 perms)

EXECUTION

** NOTE TO SPECIFIER ** - See Petersen Aluminum Corporation Installation Guide for recommended fastening patterns and installation methods. Coordinate panel installation requirements with wall covering manufacturer.

EXAMINATION

Do not begin installation until exterior walls have been properly prepared.

Verify that all exterior wall assembly construction has been completed to the point where the insulation may correctly be installed.

Verify that mechanical and electrical services in walls have been installed and tested and, if appropriate, verify that adjacent materials and finishes are dry and ready to receive insulation.

If wall assembly preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

PREPARATION

Clean surfaces thoroughly prior to installation.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

INSTALLATION

Install in accordance with manufacturer's instructions.

Install in exterior spaces without gaps or voids. Do not compress insulation.

Trim insulation neatly to fit spaces. Insulate miscellaneous gaps and voids.

Fit insulation tight in spaces and tight to exterior side of mechanical and electrical services within plane of insulation.

Insulation must be protected from open flame and stored in accordance with the manufacturer’s instructions.

Fasten composite insulation to the structural base wall. Coordinate with the cladding or wall finish manufacturer for the attachment requirements over insulation panels. Contact Petersen Aluminum Corporation for guidance when determining fastening pattern.

Install vapor retarders over insulation panels as specified in Section 07260.

Install air barriers over insulation panels as specified in Section 07270.

PAC-Shield CI is not intended to be left exposed for extended periods of time. During the time between the installation of the PAC-Shield CI Nail Base and the application of the exterior cladding it is recommended that the WRB be installed as soon as possible. If the WRB is not being installed right away it is recommended that the PAC-Shield CI Nail Base be protected from excess moisture and UV. All unfaced foam exposed directly to daylight can be taped with a compatible waterproof tape and the edges of the boards can be buttered with a compatible sealant.

PROTECTION

Protect installed products until completion of project.

Cover the top and edges of unfinished wall panel work to protect it from the weather and to prevent accumulation of water in the cores of the panels.

Wet panels shall be allowed to completely dry prior to application of vapor barrier and/or cladding.

Repair or replace damaged products before Substantial Completion.

END OF SECTION