# GUIDE SPECIFICATION

# Tite-Loc Aluminum

August 2024

## SECTION 07410- PREFORMED METAL STANDING SEAM ROOFING

– GENERAL

DESCRIPTION OF WORK

This section covers the pre-finished, pre-fabricated Architectural standing seam roof system. All metal trim, accessories, fasteners, insulation and sealants indicated on the drawings as part of this section.

Drawings and general provisions of the Contract, including general and Supplementary Conditions and Division 01 Specifications, apply to this section.

Related Work Specified Elsewhere

Roof Deck structural steel, flat roof systems, perimeter edge systems. Roof hatches, firestopping not included in this section.

SUMMARY

Section Includes

Factory formed Standing Seam metal roof panels

Related work specified elsewhere. (Note: select from the below or add appropriate sections)

Section 05100 - Structural Steel

Section 05200 or 05400 - Steel Joists

Section 07600 - Flashing and Sheet Metal

DEFINITIONS

Metal Roof Panel Assembly: Metal roof panels, attachment system components, miscellaneous metal framing, thermal, and accessories necessary for a complete weathertight roofing system.

References:

American Society for Testing and Materials (ASTM)

ASTM B209 Standard Specification for Aluminum and Aluminum-Alloy Sheet and Plate

Sheet Metal and Air Conditioning Contractors National Association (SMACNA)

SMACNA Architectural Sheet Metal Manual, 1993 edition

American Iron and Steel Institute (AISI)

AISI Cold Formed Steel Design Manual

Aluminum Association

Aluminum Design Manual

Metal Construction Association

Preformed metal Wall Guidelines

Code References

ASCE, Minimum Loads for Buildings and Other Structures

BOCA National Building Codes

UBC Uniform Building Code

SBC Standard Building Code

QUALITY ASSURANCE

Petersen Aluminum Corporation products establish a minimum of quality required. Specifier: Choose location:

Petersen Aluminum Corp, Elk Grove Village, IL, 800-323-1960

Petersen Aluminum Corp, Annapolis Junction, MD, 800-344-1400

Petersen Aluminum Corp, Tyler, TX, 800-441-8661

Petersen Aluminum Corp, Acworth, GA, 800-272-4482

Manufacturer and erector shall demonstrate experience of a minimum of five (5) years in this type of project.

Panels shall be factory-produced only. No portable, installer-owned or installer-rented  machines will be permitted.

SUBSTITUTIONS

The material, products and equipment specified in this section establish a standard for required function, dimension, appearance and quality to be met by any proposed substitution.

SYSTEM DESCRIPTION

Material to comply with ASTM B209 Standard Specification for Aluminum and Aluminum-Alloy Sheet and Plate

ROOF SYSTEM PERFORMANCE TESTING

General Performance: Metal roof panels shall comply with performance requirements without failure due to defective manufacture, fabrication, installation or other defects in construction.

Roof System shall be designed to meet Standard Building Code Wind Load requirements.

Panels to meet:

Water Penetration:  When tested per ASTM  E-283/1680 and ASTM E-331/1646 there shall be no uncontrolled water penetration  or air infiltration  through the panel joints.

Roof System shall be designed to meet a UL Class 90 wind uplift in accordance with UL standard 580 and panel system shall be ASTM 1592 Tested and approved

UL 2218 – Impact Resistance rated.

WARRANTIES

Weathertight warranty: Manufacturer’s standard form in which manufacturer agrees to repair or replace standing seam metal roof panel assemblies that fail to remain weathertight, including leaks, within specified warranty period.

Warranty Period: 20 Years from date of Substantial Completion

Finish warranty: Manufacturer’s standard form in which manufacturer agrees to repair finish or replace standing seam metal roof panels that show evidence of deterioration of factory-applied finish within specified warranty period.

Exposed Panels Finish – deterioration includes the following:

Color fading more than 5 hunter units when tested according to ASTM D 2244

Chalking in excess of a No. 8 rating when tested according to ASTM D 4214

Cracking, checking, peeling or failure of a paint to adhere to a bare metal.

Warranty Period: 30 Years from the date of substantial completion

Applicator shall furnish written warranty for a two (2) year period from date of substantial completion of building covering repairs required to maintain roof and flashings in watertight condition

SUBMITTALS

Furnish detailed drawings showing profile and gauge of exterior sheets, location and type of fasteners, location, gauges, shape and method of attachment of all trim locations and types of sealants, and any other details as may be required for a weather-tight installation.

Provide finish samples of all colors specified.

Shop drawings: Show fabrication and installation layouts of metal roof panels, metal wall panels or metal soffit panels, details of edge conditions, side-seam joints, panel profiles, corners, anchorages, trim, flashings, closures and accessories, and special details. Distinguish between factory and field-assembled work

Coordination Drawings: Roof plans, drawn to scale, on which the following are shown and coordinated with each other, base don input from installer of the items involved:

Roof panels and attachments

Metal trusses, bracings and supports

Roof-mounted items including snow guards and items mounted on roof curbs.

LEED Submittals

Product Test reports for Credit SS 7.2. For roof panels, indicating that the panels comply with Solar Reflective Index requirement

Product data for Credit MR 4.1 and credit MR 4.2: Indicating the percentages by weight of postconsumer and preconsumer recycled content for products having recycled content.

DELIVERY, STORAGE AND HANDLING

Ordering: Comply with manufacturer’s ordering instruction and lead time requirements to avoid construction delays.

Deliver components, sheets, metal roof panels and other manufactured items so as not to be damaged or deformed. Package metal roof panels for protection during transportation and handling.

Unload, store and erect metal roof panels in a manner to prevent bending, warping, twisting and surface damage.

Stack metal roof panels on platforms or pallets, covered with suitable weathertight and ventilated covering. Store metal roof panels to ensure dryness. Do not store metal roof panels in contact with other materials that might cause staining, denting or other surface damage.

Protect strippable protective coating on any metal coated product from exposure to sunlight and high humidity, except to the extent necessary for material installation.

PROJECT CONDITIONS

Weather Limitations: proceed with installation only when existing and forecasted weather conditions permit metal roof panel work to be performed.

Field Measurements: Verify actual dimensions of construction contiguous with metal roof panels by field measurements before fabrication.

COORDINATION

Coordinate sizes and locations of roof curbs, equipment supports and roof penetrations with actual equipment provided.

Coordinate metal roof panels with rain drainage work, flashing, trim and construction of decks, parapet walls and other adjoining work to provide a leakproof, secure and noncorrosive installation.

– PRODUCTS

PANEL DESIGN

General: Provide factory-formed metal roof panels designed to be installed by lapping and interconnecting raised side edges of adjacent panels with joint type indicated and mechanically attaching panels to supports using concealed clips in side laps. Include clips, cleats, pressure plates and accessories required for a weathertight installation.

Roof panels shall be standing seam Tite Loc Plus, in {Specifier choose from)  18” 16” or 12” widths with 2” seams that are mechanically seamed together at 180 degrees.

Panels to be produced with Factory supplied hot melt mastic in the seams.

Panels to be produced:. Specifier note: Choose from panel conditions below:

Smooth – Note this is factory standard if other not indicated

With Striations

With striations with pencil ribs (Acworth factory only)

Panels to be designed for attachment with concealed fastener clips, spaced as required by the manufacturer to provide for both positive and negative design loads, while allowing for the expansion and contraction of the entire roof system resulting from variations in temperature.

Forming: Use continuous end rolling method. No end laps on panels. No portable rollforming machines will be permitted on this project, no installer-owned or installer-rented machines will be permitted. It is the intent of the Architect to provide Factory-Manufactured panel systems only for this project.

ACCEPTABLE MANUFACTURERS

This project is detailed around the Tite Loc Plus Panel of Petersen Aluminum Corporation.

MATERIALS AND FINISHES

Preformed roofing panels shall be fabricated of (Specifier Note – choose from) .032 thickness 3105-H14 aluminum or .040 thickness 3105-H14 aluminum.

Color shall be PAC-CLAD ____________________.(Specifier – choose finish from available colors shown by gauge on PAC color chart)

Finish shall be Kynar 500 or Hylar 5000 Fluorocarbon coating with a top side film thickness of 0.70 to 0.90 mil over a 0.25 to 0.3 mil prime coat to provide a total dry film thickness of 0.95 to 1.25 mil, to meet AAMA 621. Bottom side shall be coated with a primer with a dry film thickness of 0.25 mil. Finish shall conform to all tests for adhesions, flexibility and longevity as specified by Kynar 500 or Hylar 5000 finish supplier.

If Strippable coating to be applied on the pre-finished panels to the top side to protect the finish during fabrication, shipping and handling, film shall be removed before installation.

Trim: Trim shall be fabricated of the same material and finish to match the profile, and will be press broken in lengths of 10 to 12 feet. Trim shall be formed only by the manufacturer or their approved dealer. Trim to be erected in overlapped condition. Use lap strips only as indicated on drawings. Miter conditions shall be factory welded material to match the sheeting.

Closures: use composition or metal profiled closures at the top of each elevation to close ends of the panels. Metal closures to be made in the same material and finish as face sheet.

Accessories/Fasteners: Fasteners shall be of type, material, size, corrosion resistance, holding power and other properties required to fasten miscellaneous framing members to substrates. Accessories and their fasteners shall be capable of resisting the specified design wind uplift forces and shall allow for thermal movement of the roof panel system. Exposed fasteners shall not restrict free movement of the roof panel system resulting from thermal forces, except at designed points of roof panel fixity

Substrate shall be:(Specifier: choose from)

Plywood

ISO

Nailbase

Roofing Underlayment

On all surfaces to be covered with roofing material, furnish and install a 40 mil “Peel & Stick membrane”, required as outlined by metal panel manufacturer. Membrane to be a minimum of 40 mil thickness, smooth, non-granular, high temperature. Basis of design: Carlisle WIP 300 HT High Temperature Protection Self Adhering Roofing Underlayment. Other acceptable manufacturers include:

W.R Grace “Ice & Water Shield”

Interwrap Titanium PSU-30

Tamko TW Tile and Metal Underlayment

Underlayment shall be laid in horizontal layers with joints lapped toward the eaves a minimum of 6”, and well secured along laps and at ends as necessary to properly hold the felt in place. All underlayment shall be preserved unbroken and whole.

Peel and Stick Underlayment shall lap all hips and ridges at least 12” to form double thickness and shall be lapped 6” over the metal of any valley or built-in gutters and shall be installed as required by the Standing Seam Panel Manufacturer to attain the desired 20 Year Weathertightness Warranty.

Sealants

Provide two-part polysulfide class B non-sag type for vertical and horizontal joints or

One part polysulfide not containing pitch or phenolic extenders or

Exterior grade silicone sealant recommended by roofing manufacturer or

One part non-sag, gun grade exterior type polyurethane recommended by the roofing manufacturer.

FABRICATION

Comply with dimensions, profile limitations, gauges and fabrication details shown and if not shown, provide manufacturer’s standard product fabrication.

Fabricate components of the system in factory, ready for field assembly.

Fabricate components and assemble units to comply with fire performance requirements specified.

Apply specified finishes in conformance with manufacturer’s standard, and according to manufacturer’s instructions.

– EXECUTION

INSPECTION

Examine alignment of structural steel and related supports, primary and secondary roof framing, solid roof sheathing, prior to installation.

For the record, prepare written report, endorsed by installer, listing conditions detrimental to performance of the Work.

Proceed with installation only after unsatisfactory conditions have been corrected.

FASTENERS

Secure units to supports

Place fasteners as indicated in manufacturer’s standards.

INSTALLATION

Panels shall be installed plumb and true in a proper alignment and in relation to the structural framing. The erector must have at least five years successful experience with similar applications.

Install metal panels, fasteners, trim and related sealants in accordance with approved shop drawings and as may be required for a weather-tight installation.

Remove all strippable coating and provide a dry-wipe down cleaning of the panels as they are erected.

DAMAGED MATERIAL

Upon determination of responsibility, repair or replace damaged metal panels and trim to the satisfaction of the Architect and Owner.

END OF SECTION