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GUIDE SPECIFICATION
Corr-Lok, Design-Lok, Max-Lok, Mesa-Lok, 
Mesa-Lok HSE, Shadow-Lok

October 2024
SECTION 07 42 13- INSULATED METAL WALL PANELS
- GENERAL
Summary
The contract drawings indicate the extent and general details of the walls. This section includes requirements for the factory-formed, pre-insulated, metal, wall panel cladding system and the corresponding metal flashings, sealants, fasteners, clips and other accessories.
Related Sections
Section 05 40 00 - Cold Formed Metal Framing
Section 06 10 00 - Rough Carpentry
Section 07 21 00 - Thermal Insulation
Section 07 25 00 - Weather Barriers
Section 07 27 00  -  Air Barriers
Section 07 62 00 - Sheet Metal Flashing and Trim
Section 07 92 99 - Joint Sealants
References
AISC - Steel Construction Manual – 15th Edition
AISI - North American Specification for the Design of Cold-Formed Structural Members, 2016
ASCE 7 - Minimum Design Loads for Buildings and Other Structures
ASTM
ASTM C 518-10 Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus
ASTM C 1363-05 Standard Test Method for Thermal Performance of Building Materials and Envelope Assemblies by Means of a Hot Box Apparatus
ASTM C 273-07 Standard Test Method for Shear Properties of Sandwich Core Materials
ASTM D 1621-10 Standard Test Method for Compressive Properties of Rigid Cellular Plastics
ASTM D 1623-09 Standard Test Method for Tensile and Tensile Adhesion Properties of Rigid Cellular Plastics
ASTM D 1622-08 Standard Test Method for Apparent Density of Rigid Cellular Plastics
ASTM D 6226-10 Standard Test Method for Open Cell Content of Rigid Cellular Plastics
ASTM E 72-10 Standard Test Methods of Conducting Strength Tests of Panels for Building Construction
ASTM E 84-10b Standard Test Method of Surface Burning Characteristics of Building Materials
ASTM E 283-04 Standard Test Method for Determining Rate of Air Leakage Through Exterior Windows, Curtain Walls and Doors Under Specified Pressure Differences Across the Specimen
ASTM E 331-00 Standard Test Method for Water Penetration of Exterior Windows, Skylights, Doors, and Curtain Walls by Uniform Static Air Pressure Difference
ASTM E 1592-05 Standard Test Method for Structural Performance of Sheet Metal Roof and Siding Systems by Uniform Static Air Pressure Difference
FM Global
FM 4880 Approval Standard for Class 1 Fire Rating of Insulated Wall or Wall and Roof/Ceiling Panels, Interior Finish Materials or Coatings and Exterior Wall Systems
4881 Approval Standard for Class 1 Exterior Wall Systems
International Building Code (IBC)
Submittals
Manufacturer’s product literature. Include product data and installation instructions.
Manufacturer’s written installation instructions: Provide manufacturer’s written instructions to installer, marked to show component installation; Where instructions allow installation options, indicate option for use.
Shop drawings showing elevations, panel layout and calling out panel profile, thickness, gauge, width, finish and texture. 
The drawings shall also illustrate product components including fasteners, clips, sealants, trims and any other necessary accessories.
Engineering package illustrating the panels will resist the code stipulated loads.
Color chip and/or chart.
Samples: 12” long sample of wall panel. Provide color ships for selection of color and sheen. Provide (2) 3” x 5” finish samples in color selected.
Installation instructions.
Sample warranties (substrate and finish).
Letter of Certification stating that all parts of this specification were satisfied.
Delivery, Storage and Handling
Deliver panels in the original manufacturer’s weather-resistant, shrink-wrapped packaging with clearly marked, weather-resistant labeling.
Store the panels in a clean, level, protected and sufficiently compacted area. Provide ventilation if the bundles are exposed to moisture; further, elevate one end of the bundle to ensure adequate runoff. Do not stack more than two bundles high. Stack material to prevent twisting, bending, abrasion, scratching and denting.
Use proper care in unloading, storing and installing the wall panels. Handle panels in a fashion that will not bend, dent, scratch or otherwise damage the product.
Refer to the PAC-CLAD IMP Insulated Metal Panel Handling & Maintenance Guide for more specific information regarding handling, storage, strippable film, steel debris, corrosion, cleaning and field painting.
Project Conditions
Weather limitations: Proceed with installation only when existing and forecasted weather conditions permit assembly of metal panels to be performed according to manufacturer’s written instructions and warranty requirements.
Warranty
The manufacturer warrants the panels as free of defects in material and workmanship for a period of (2) years from the date of production. This excludes the material coatings and finishes which are covered under separate warranties.
The manufacturer warrants the GALVALUME® substrate for a period of 20-years subject to the terms and conditions set forth in the manufacturer’s GALVALUME® 20-Year Limited Warranty.
The manufacturer warrants the Kynar 500® coating system for a period of 25-years subject to the terms and conditions set forth in the manufacturer’s Coating System Limited Warranty.
The installer warrants the panels as free of defects in material installation and workmanship for a period of (2) years from the date of substantial completion.
Maintenance
Keep the interior and exterior panel surfaces clean. Immediately remove dust, dirt, mud, mortar, chalk, excess sealants or any other type of foreign substance from the panel surfaces.
Refer to the PAC-CLAD IMP Handling & Maintenance Guide for more specific information regarding handling, storage, strippable film, steel debris, corrosion, cleaning and field painting.
- PRODUCT
Manufacturer/Supplier 
Petersen Aluminum Corporation
1005 Tonne Road
Elk Grove Village, IL 60007
Phone: (800) PAC-CLAD
Fax: (800) 722-7150
E-mail: info@pac-clad.com
Internet: www.pac-clad.com
System:
Prefinished metal wall panels, subgirt framing assembly, fasteners and anchors supported by framing or other substrate provided by others; site assembled.
Components / Materials:
Panels
Type: Insulated Metal Wall Panels consisting of roll-formed interior and exterior profiles chemically bonded to a continuously, foamed-in-place, polyisocyanurate, insulating core.
Classification
FM Global 4880 Approved Class 1 Fire Rated Insulated Wall/Ceiling System.
FM Global 4881 Approved Class 1 Exterior Wall System.
State of Florida Approved Building Product
Miami Dade County Approved
Design-Lok
Panel Use: Exterior Wall
Coverage Width: 42-inch
Thickness: 2, 2.5, 3, 4-inch
Length: 8’-0” to 40’-0”
Exterior Gauge: 26, 24
Interior Gauge: 26
Exterior Substrate: Galvalume®, G90
Interior Substrate: Galvalume®, G90, Stainless Steel
Exterior Finish: Siliconized Polyester, low-gloss PVDF 
Interior Finish: Polyester, Siliconized Polyester, Plastisol (PVC) 
Exterior Texture: Heavy Embossed
Interior Texture: Embossed, smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam 
R-Value: R-8 per inch of thickness (nominal)
Max-Lok
Panel Use: Partition Wall, Liner Wall, Tee Supported Ceiling
Coverage Width: 45-inch
Thickness: 3, 4, 5, 6-inch
Length: 8’-0” to 53’-0”
Exterior Gauge: 26
Interior Gauge: 26
Exterior Substrate: Galvalume®
Interior Substrate: Galvalume®
Exterior Finish: Polyester, Siliconized Polyester, Plastisol (PVC) 
Interior Finish: Polyester, Siliconized Polyester, Plastisol (PVC) 
Exterior Texture: Embossed, Smooth
Interior Texture: Embossed, Smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam
 R-Value: R-8 per inch of thickness (nominal)
Mesa-Lok
Panel Use: Exterior Wall, Partition Wall, Liner Wall, Ceiling
Coverage Width: 42-inch
Thickness: 2, 2.5, 3, 4, 5, 6-inch
Length: 8’-0” to 53’-0”
Exterior Gauge: 26, 24, 22
Interior Gauge: 26
Exterior Substrate: Galvalume®, G90, Stainless Steel
Interior Substrate: Galvalume®, G90, Stainless Steel
Exterior Finish: Polyester, Siliconized Polyester, low-gloss PVDF, Plastisol (PVC)
Interior Finish: Polyester, Siliconized Polyester, Plastisol (PVC)
Exterior Texture: Embossed, Smooth 
Interior Texture: Embossed, Smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam
R-Value: R-8 per inch of thickness (nominal)
Mesa-Lok HSE
Panel Use: Exterior Wall
Coverage Width: 42-inch
Thickness: 2, 2.5, 3, 4, 5, 6-inch
Length: 8’-0” to 53’-0”
Exterior Gauge: 26, 24
Interior Gauge: 26
Exterior Substrate: Galvalume®, G90
Interior Substrate: Galvalume®, G90, Stainless Steel
Exterior Finish: Siliconized Polyester, low-gloss PVDF 
Interior Finish: Polyester, Siliconized Polyester, Plastisol (PVC)
Exterior Texture: Heavy Stucco Embossed (HSE)
Interior Texture: Embossed, Smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam
R-Value: R-8 per inch of thickness (nominal)
Shadow-Lok
Panel Use: Exterior Wall
Coverage Width: 42-inch
Thickness: 2, 2.5, 3, 4, 5, 6-inch
Length: 8’-0” to 53’-0”
Exterior Gauge: 26, 24, 22
Interior Gauge: 26
Exterior Substrate: Galvalume®, G90
Interior Substrate: Galvalume®, G90, Stainless Steel
Exterior Finish: Siliconized Polyester, low-gloss PVDF 
Interior Finish: Polyester, Siliconized Polyester, Plastisol (PVC)
Exterior Texture: Embossed, Smooth
Interior Texture: Embossed, Smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam
R-Value: R-8 per inch of thickness (nominal)
Corr-Lok
Panel Use: Exterior Wall
Coverage Width: 42-inch
Thickness: 2, 2.5, 3, 4-inch
Length: 8’-0” to 40’-0”
Exterior Gauge: 24, 22
Interior Gauge: 26
Exterior Substrate: Galvalume®, G90
Interior Substrate: Galvalume®, G90
Exterior Finish: Siliconized Polyester, low-gloss PVDF
Interior Finish: Polyester, Siliconized Polyester
Exterior Texture: Embossed, Smooth
Interior Texture: Embossed, Smooth
Joint: Green-Lock, offset double tongue-and-groove
Core: Continuously poured-in-place polyisocyanurate insulating foam
R-Value: R-8 per inch of thickness (nominal)
Flashing
Match all flashings and trims with the adjacent panels in material gauge and finish. Install these trims per the panel manufacturer’s details.
Accessories
Clips
14-ga., 4”, 5-hole wall panel clip (AC-01)
14-ga., 8”, 3-hole wall panel clip (BAC-08)
12-ga., 12”, 3-hole wall panel clip (BAC-12)
Fasteners – Self-Drilling or Self-Tapping, Hex Head of appropriate length.
Closures – UV resistant per the manufacturer’s details (if necessary).
Sealers
Tube Sealants
Non-skinning
Polyurethane
Tape Sealants 
Butyl
System Performance
Structural
Load Capacity - Determine positive and negative load resistance based on tests conducted in accordance with ASTM E 1592 and/or ASTM E 72.
Load Calculation – Dictated by ASCE 7 16 and the building dimensions
Deflection Limit – per code or L/180, whichever is greater.
Connection – Designed considering the load (psf), tributary area (sqft), ultimate fastener pullout/pullover (lbs.) and appropriate factor of safety.
Factor of Safety (panel): 2.0
Factor of Safety (fasteners)
Two fasteners into steel:	2.25
One fastener into steel:	3.00
One or two fasteners into masonry:	4.00
Material Thickness – The delivered material thickness (steel) shall be within 95% of the design thickness.
Impact Resistance
Very severe hail (VSH) resistance when tested in accordance with FM Standard 4881.
Large Missile Impact tested in accordance with Miami Dade County TAS 201.
Water-tightness
Verify the panels allow no uncontrolled water penetration when subjected to a pressure differential of - 20-psf when tested in accordance with ASTM E 331.
Air-tightness
Verify the panels allow no more than 0.0011 cfm/sf at a pressure differential of +/- 20-psf when tested in accordance with ASTM E 283.
Metal Facing to Foam Core Bond Strength
Fatigue – Upon being subjected to two-million alternating cycles of L/180 deflection, the panels shall exhibit no evidence of delamination of the fascia or liner elements, cracking of the foam core, or permanent set.
Freeze/Heat Cycling – At the conclusion of twenty-one (21) eight-hour temperature cycles (-20° F to 180° F), the panels shall exhibit no evidence of delamination, blistering or permanent set.
Humidity – After enduring 1200 hours of 93% humidity at a temperature of 158° F, the panels shall exhibit no evidence of delamination, blistering or interface corrosion.
Autoclave – When exposed to 218°F and a pressure of 2-psig for 2-1/2 hours, the panels shall exhibit no delamination of the foam core from the metal skins.
Energy Efficiency
When tested in accordance with ASTM C 518 the panels provide a K-factor of: 0.139 Btu-in/hr-ft2-F° @ 75° F mean temperature (R-7.20) and 0.129 Btu-in/hr-ft2-F° @ 35° F mean temperature (R-7.75).
Fire Safety
The panels will be classified according to FM 4880 for unlimited height and NFPA 285.
Surface Burning Characteristics
Verify the panels have a maximum Flame Spread of 25 and maximum Smoke Developed of 450 when tested in accordance with ASTM E84.
Material Compatibility
Prevent galvanic action of dissimilar metals. This includes but is not limited to any direct contact of panels and/or trim with treated lumber or copper lightening attenuation equipment or indirect contact constituted by water runoff from HVAC drain-lines, etc.
- EXECUTION
General
The Contractor, upon entering into a contract to erect the Wall Panel System, claims itself competent in the erection of these systems and is responsible for complying with all applicable local federal and state construction and safety regulations, including OSHA regulations.
Preparation
Contractor - Before wall panel installation begins, meticulously review and accept the shop drawings as correct.
Examination
Shipment - Immediately upon delivery of the wall panels and accessories, crosscheck the delivered materials against the shipper to insure a complete shipment.
Substrate – Before installation begins, inspect and accept the structure with regard to plumb, level and true. The maximum deviation of steel alignment shall be limited to 0 (+\-) 3/16” from the control with a 1/8” maximum change in deviation for any member of any 10-ft panel run. The Contractor shall not proceed with installation if the structural steel is not within the specified tolerances.
Panels – During installation, examine the individual panels. Immediately notify the manufacturer of any panel defects. Do not install defective panels.
Installation
Panels
Install in accordance with the manufacturer’s recommended procedures, details and the construction drawings. Install the panels plumb, level and true. If necessary, make panel cuts with a “metal cutting” circular saw.
Fasteners
Install fasteners in the locations shown on the construction drawings. Take care not to overdrive fasteners. Replace stripped fasteners by installing a new fastener in a different location.
Trim
Install the flashing true-to-line and level or plumb and in accordance with the manufacture’s details and the construction drawings.
Sealants
Before sealants are applied, clean and prime the surfaces according to the sealant manufacturer’s guidelines. Locate the sealants per the manufacturer’s details and the shop drawings without skips or voids.
Installation Guide:
Refer to the PAC-CLAD IMP Installation Guide for specific information regarding accountability, conditions, heavy equipment, verification of structure, alignment, side-joints, vapor barrier, sealants, field applied insulation, threaded fasteners, strippable film, field cutting, appearance, general installation sequence and details.
Do not place utility penetrations through panel seams.
Do not allow panels or trim to come into contact with dissimilar materials. Protect from water run-off from these materials.
Protection
Protect metal wall panels until completion of project.
Remove any and all strippable films either prior to or directly following installation. Take measures to avoid exposure of the film to direct sunlight for more than 24 hours.
Cleaning
Touch Up – “Touch up” minor damage to factory applied finishes using factory approved, matching coatings provided by the manufacturer.
Soap - If necessary, clean panel surfaces with a combination of water and a light detergent.
END OF SECTION
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